## Slide 1
Mechanical Properties of Materials

## Slide 2
Stress-strain behavior
Stress = Force/cross section area
Force can be applied on materials in tension, compression, shear or combination of any combination of these forces
Deformation of the material in response to applied force is called strain
Shear Modulus (G) = (F/A)/(l/l) , Shear strain - l/l
For isotropic materials:
E = 2G(1+)
 is Poisson’s ratio
Poisson’s ratio is defined as negative ratio of the transverse strain to longitudinal strain
(a) Schematic illustration of how a tensile load produces an elongation. Dashed lines represent the shape before deformation; solid lines, after deformation. (b) Schematic illustration of how a compressive load produces contraction (c) Schematic representation of shear strain , where =tan. (d) Schematic representation of torsional deformation (i.e., angle of twist ) produced by an applied torque T.

## Slide 3
Stress-strain plot
Yield point
Hooke’s law – Strain is proportional to applied stress in elastic region.
E=/
E is called modulus of elasticity or Young’s modulus
In plastic region deformation are permanent
Tensile strength – the peak stress
Fracture strength – the stress where facture occurs

## Slide 4
Schematic representation of the apparatus used to conduct tensile stress–strain tests. The specimen is elongated by the moving crosshead; load cell and extensometer measure, respectively, the magnitude of the applied load and the elongation.
Problem: A piece of copper originally 305 mm long is pulled in tension with a stress of 276 MPa (40,000 psi). If the deformation is entirely elastic, what will be the resultant elongation? (Elastic modulus of copper is 110 GPa)
STRESS–STRAIN BEHAVIOR
Schematic stress–strain diagram showing linear elastic deformation for loading and unloading cycles.

## Slide 5
Plastic Deformation
Typical engineering stress– strain behavior to fracture, point F. The tensile strength TS is indicated at point M. The circular insets represent the geometry of the deformed specimen at various points along the curve.
Typical stress–strain behavior for a metal showing elastic and plastic deformations, the proportional limit P, and the yield strength as determined using the 0.002 strain offset method.
The stress corresponding to the intersection of this line and the stress–strain curve as it bends over in the plastic region is defined as the yield strength

## Slide 6
Ductility is another important mechanical property. It is a measure of the degree of plastic deformation that has been sustained at fracture. A material that experiences very little or no plastic deformation upon fracture is termed brittle.
Schematic representations of tensile stress–strain behavior for brittle and ductile materials loaded to fracture.
Ductility may be expressed quantitatively as either percent elongation or percent reduction in area.

## Slide 7
Typical Mechanical Properties of Several Metals and Alloys in an Annealed State

## Slide 8
Elastic and plastic deformation

## Slide 9
Resilience is the capacity of a material to absorb energy when it is deformed elastically and then, upon unloading, to have this energy recovered.The associated property is the modulus of resilience, which is the strain energy per unit volume required to stress a material from an unloaded state up to the point of yielding. Computationally, the modulus of resilience for a specimen subjected to a uniaxial tension test is just the area under the engineering stress–strain curve taken to yielding
Assuming linear elastic region:

## Slide 10
Toughness is a mechanical term that is used in several contexts; loosely speaking, it is a measure of the ability of a material to absorb energy up to fracture.

## Slide 11
HARDNESS
Another mechanical property that may be important to consider is hardness, which is a measure of a material’s resistance to localized plastic deformation (e.g., a small dent or a scratch).
Early hardness tests were based on natural minerals with a scale constructed solely on the ability of one material to scratch another that was softer.
A qualitative and somewhat arbitrary hardness indexing scheme was devised, termed the Mohs scale, which ranged from 1 on the soft end for talc to 10 for diamond.
The Rockwell tests constitute the most common method used to measure hardness because they are so simple to perform and require no special skills.
It permits the testing of virtually all metal alloys (as well as some polymers).
Indenters include spherical and hardened steel balls having diameters of 1/16, 1/8, 1/4 and ½ in. (1.588, 3.175, 6.350, and 12.70 mm), and a conical diamond (Brale) indenter, which is used for the hardest materials.
With this system, a hardness number is determined by the difference in depth of penetration resulting from the application of an initial minor load followed by a larger major load; utilization of a minor load enhances test accuracy.

## Slide 12
Knoop and Vickers Microindentation Hardness Tests
Two other hardness-testing techniques are Knoop and Vickers.
For each test a very small diamond indenter having pyramidal geometry is forced into the surface of the specimen. Applied loads are much smaller than for Rockwell and Brinell, ranging between 1 and 1000 g.
The resulting impression is observed under a microscope and measured; this measurement is then converted into a hardness number.
Brinell Hardness Tests1
In Brinell tests, as in Rockwell measurements, a hard, spherical indenter is forced into the surface of the metal to be tested. The diameter of the hardened steel (or tungsten carbide) indenter is 10.00 mm (0.394 in.).
Standard loads range between 500 and 3000 kg in 500-kg increments; during a test, the load is maintained constant for a specified time (between 10 and 30 s).
Harder materials require greater applied loads. The Brinell hardness number, HB, is a function of both the magnitude of the load and the diameter of the resulting indentation

## Slide 13
Hardness-Testing Techniques

## Slide 14
Any fracture process involves two steps—crack formation and propagation—in response to an imposed stress.
The mode of fracture is highly dependent on the mechanism of crack propagation.
Ductile fracture is characterized by extensive plastic deformation in the vicinity of an advancing crack.
On the other hand, for brittle fracture, cracks may spread extremely rapidly, with very little accompanying plastic deformation.
Ductile fracture is almost always preferred for two reasons. First, brittle fracture occurs suddenly and catastrophically without any warning; this is a consequence of the spontaneous and rapid crack propagation.
On the other hand, for ductile fracture, the presence of plastic deformation gives warning that fracture is imminent, allowing preventive measures to be taken.
Second, more strain energy is required to induce ductile fracture inasmuch as ductile materials are generally tougher.
Under the action of an applied tensile stress, most metal alloys are ductile, whereas ceramics are notably brittle, and polymers may exhibit both types of fracture.
FUNDAMENTALS OF FRACTURE

## Slide 15
DUCTILE FRACTURE
Highly ductile fracture in which the specimen necks down to a point.
Moderately ductile fracture after some
necking.
(c) Brittle fracture without any plastic deformation.
The most common type of tensile fracture profile for ductile metals is that represented in Figure b, where fracture is preceded by only a moderate amount of necking.

## Slide 16
The fracture process normally occurs in several stages.
First, after necking begins, small cavities, or microvoids, form in the interior of the cross section, as indicated in Figure b.
Next, as deformation continues, these microvoids enlarge, come together, and coalesce to form an elliptical crack, which has its long axis perpendicular to the stress direction.
The crack continues to grow in a direction parallel to its major axis by this microvoid coalescence process (Figure c).
Finally, fracture ensues by the rapid propagation of a crack around the outer perimeter of the neck (Figure d), by shear deformation at an angle of about 450 with the tensile axis—this is the angle at which the shear stress is a maximum.
Sometimes a fracture having this characteristic surface contour is termed a cup-and-cone fracture because one of the mating surfaces is in the form of a cup, the other like a cone.

## Slide 17
(a) Cup-and-cone fracture in aluminum. (b) Brittle fracture in a mild steel.
(a)
(b)

## Slide 18
The measured fracture strengths for most brittle materials are significantly lower than those predicted by theoretical calculations based on atomic bonding energies.
This discrepancy is explained by the presence of very small, microscopic flaws or cracks that always exist under normal conditions at the surface and within the interior of a body of material.
These flaws are a detriment to the fracture strength because an applied stress may be amplified or concentrated at the tip, the magnitude of this amplification depending on crack orientation and geometry.
(a) The geometry of surface and internal cracks. (b) Schematic stress profile along the line X–X’ in (a), demonstrating stress amplification at crack tip positions.
PRINCIPLES OF FRACTURE MECHANICS

## Slide 19
As indicated by this profile, the magnitude of this localized stress diminishes with distance away from the crack tip.
At positions far removed, the stress is just the nominal stress or the applied load divided by the specimen cross-sectional area (perpendicular to this load).
Due to their ability to amplify an applied stress in their locale, these flaws are sometimes called stress raisers.
If it is assumed that a crack is similar to an elliptical hole through a plate, and is oriented perpendicular to the applied stress, the maximum stress m, occurs at the crack tip and may be approximated by:
Where 0 is the magnitude of the nominal applied tensile stress, t is the radius of curvature of the crack tip, and a represents the length of a surface crack, or half of the length of an internal crack.
Sometimes m /0 the ratio is denoted as the stress concentration factor Kt

## Slide 20
Furthermore, the effect of a stress raiser is more significant in brittle than in ductile materials.
For a ductile material, plastic deformation ensues when the maximum stress exceeds the yield strength. This leads to a more uniform distribution of stress in the vicinity of the stress raiser and to the development of a maximum stress concentration factor less than the theoretical value.
Such yielding and stress redistribution do not occur to any appreciable extent around flaws and discontinuities in brittle materials; therefore, essentially the theoretical stress concentration will result.
Using principles of fracture mechanics, it is possible to show that the critical stress c required for crack propagation in a brittle material is described by the expression
Where:
E = Elastic of modulus
s = specific surface energy
a = one half the length of an internal crack
All brittle materials contain a population of small cracks and flaws that have a variety of sizes, geometries, and orientations. When the magnitude of a tensile stress at the tip of one of these flaws exceeds the value of this critical stress, a crack forms and then propagates, which results in fracture.

## Slide 21
Problem: A relatively large plate of a glass is subjected to a tensile stress of 40 MPa. If the specific surface energy and modulus of elasticity for this glass are 0.3 J/m2 and 69 GPa, respectively, determine the maximum length of a surface flaw that is possible without fracture.
Fracture Toughness
Furthermore, using fracture mechanical principles, an expression has been developed that relates this critical stress for crack propagation (c ) and crack length (a) as:
In this expression Kc is the fracture toughness, a property that is a measure of a material’s resistance to brittle fracture when a crack is present.
Worth noting is that has the unusual units of MPam. Furthermore, Y is a dimensionless parameter or function that depends on both crack and specimen sizes and geometries, as well as the manner of load application.
Relative to this Y parameter, for planar specimens containing cracks that are much shorter than the specimen width, Y has a value of approximately unity.

## Slide 22
Fatigue is a form of failure that occurs in structures subjected to dynamic and fluctuating stresses (e.g., bridges, aircraft, and machine components).
Under these circumstances it is possible for failure to occur at a stress level considerably lower than the tensile or yield strength for a static load.
Fatigue is important inasmuch as it is the single largest cause of failure in metals, estimated to comprise approximately 90% of all metallic failures; polymers and ceramics (except for glasses) are also susceptible to this type of failure.
Fatigue failure is brittle like in nature even in normally ductile metals, in that there is very little, if any, gross plastic deformation associated with failure.
The process of fatigue failure is characterized by three distinct steps:
crack initiation, wherein a small crack forms at some point of high stress concentration;
crack propagation, during which this crack advances incrementally with each stress cycle; and
final failure, which occurs very rapidly once the advancing crack has reached a critical size.
Fatigue

## Slide 23
Viscoelasticity
Viscoelastic materials are those for which the relationship between stress and strain depends on time.
In such material the stiffness will depend on rate of application of force or load.
The stored mechanical energy will be dissipated as heat in the deformation of viscoelastic materials.
All materials exhibit some viscoelastic behavior
Materials such as polymers, wood, and human tissue display significant viscoelalstic effects.

## Slide 24
Mechanical models for Viscoelastic materials
The models consist of springs, which are purely elastic and dashpots, which are purely viscous.
In spring stress is proportional to strain:
=k
K is spring constant
In dashpot stress is proportional to time derivative of strain:
=d/dt
 (eta) is viscosity

## Slide 25
Mechanical models for Viscoelastic materials
Voigt model:
total = spring + dashpot
total = k + d/dt
Problem: A stress of 1 MPa was required to stretch a 2 cm aorta strip to 2.3 cm. After an hour in the same stretched position, the strip exerted a stress of 0.75 MPa. Assume the mechanical property of the aorta did not wary appreciably during experiment.
a. Determine relaxation time (τ = η/E) using Maxwell model.
b. What stress would be exerted by the aorta strip in the same stretched position after five hours?
At t = 0, σ = 1 MPa
At t = 1 hr, σ = 0.75 MPa
Maxwell model:
total = spring + dashpot
total = /k + dashpot
Taking derivative of both side: